| Confidentiality Level |  | PU - Publish | TC ID / Revision |  | 00327274/D |
| --- | --- | --- | --- | --- | --- |
| Document Status |  | Document Released | Document No. |  | N/A |
| OBS code |  | 863 |  |  |  |
| PBS codes |  | E.E5.MSE. |  |  |  |
| Project branch |  | Engineering & Scientific documents (E&S) |  |  |  |
| Document Type |  | Specification (SP) |  |  |  |
| [RSD Product Category B] Uncoated Mirror Substrate TM-45 with a hole for 30 J, 30 fs @ 810 nm petawatt laser L3 Beam Transport in ELBA Beamline [TP21_054] Keywords n/a |  |  |  |  |  |
|  | Position |  |  | Name |  |
| Responsible person | Leader of Electron Acceleration Group |  |  | Gabriele Maria Grittani |  |
| Prepared by | Research Assistant |  |  | Lorenz Sebastian |  |

| RSS History |  |  |  |
| --- | --- | --- | --- |
| RSS TC ID/revision | RSS - Date of Creation | RSS - Date of Last Modification | Systems Engineer |
| 0023486/A.001 | 3.2.2022 | 3.2.2022 | J. Adamec |
| 0023486/B.001 | 14.2.2022 | 14.2.2022 | J. Adamec |

| Reviewed By |  |  |  |
| --- | --- | --- | --- |
| Name (reviewer) | Position (reviewer) | Date | Signature (approver) |
| Alexander Molodozhentsev | Group Leader of LUIS Beamline | Noticed (category B) |  |
| Gabriele Maria Grittani | Leader of Electron Acceleration Group | Noticed (category B) |  |
| Jaroslav Nejdl | Leader of X-ray Sources Group | Noticed (category B) |  |
| Adam Wolf | Engineering Support Group Leader | Noticed (category B) |  |
| Martin Laub | Head of department of Construction and Design Support | Noticed (category B) |  |
| Pavel Bakule | Group Leader of L1 Allegra Laser | Noticed (category B) |  |
| Veronika Olšovcová | Group Leader of Safety | Noticed (category B) |  |
| Daniel Kramer | Group Leader of Optical Materials Development | Noticed (category B) |  |
| Viktor Fedosov | Group Leader of Quality and Planning | Noticed (category B) |  |
| Radek Toman | Legal Group Leader | Noticed (category B) |  |

| Approved by |  |  |  |
| --- | --- | --- | --- |
| Name (approver) | Position (approver) | Date | Signature (approver) |
| Gabriele Maria Grittani | Leader of Electron Acceleration Group | 9.2.2022 |  |

| Revision History |  |  |  |  |
| --- | --- | --- | --- | --- |
| Revision Number | Revision Made by | Date of Revision | Revision description | TC Revision |
| 1 | Lorenz Sebastian | 2.2.2022 | Draft preparation | A |
| 2 | J. Adamec | 3.2.2022 | Praparation for review | B |
| 3 | J. Adamec | 9.2.2022 | Final version | C |
| 4 | J. Adamec / S. Lorenz | 14.2.2022 | Final version | D |

Table of Content

1. Introduction	4

1.1. Purpose	4

1.2. Scope	4

1.3. Terms, Definitions and Abbreviations	4

1.4. Reference documents	4

1.5. References to standards	4

2. Functional, Performance and Design requirements	5

2.1. General requirements	5

2.2. Marking	5

3. Packaging and transport requirements	6

3.1. General requirements	6

3.2. Transport	6

4. Quality control	6

4.1. Quality Reports (QRs)	6

4.2. Documentation and data control	7

4.3. Nonconformity Control System	7

4.4. Phasing of the delivery	7

4.4.1. Manufacturing	7

4.4.2. Acceptance	8

# Introduction

## Purpose

This Requirements Specification Document (RSD) lists the technical requirements and constraints on products applying in ELBA beamline in the ELI project. This leads to the identification of interfaces with the ELI science-based technology. This RSD also acts as the parent document for the technical requirements that need to be addressed in lower-level design description documents (see chapter 1.4).

## Scope

This RSD contains all of the technical requirements: functional, performance and design, delivery, safety and quality requirements for the following product (tender number – TP21_054): Uncoated Turning Mirror Substrate with a hole for ELI L3 laser (further referred to as “Mirror substrate”).

The product will be located in the E5 experimental hall after coating. This Mirror substrate is registered in the PPS software under the following PBS code: E.E5.MSWH.

## Terms, Definitions and Abbreviations

For the purpose of this document, the following abbreviated terms are applied:

| Abbreviation | Meaning |
| --- | --- |
| CA | Contracting Authority (Institute of Physics CAS) |
| ELI | Extreme Light Infrastructure |
| NCR | Nonconformity Report |
| QR | Quality Report |
| RA2 | Research activity 2 |
| RD | Reference Document |
| RMS | Root Mean Square |
| ELBA | Electron beam accelerator |
| RSD | Requirements Specification Document |

## Reference documents

| Number of doc. | Title of Document/File |
| --- | --- |
| RD-01 | TC ID: 00327274 - L3-160mm hole BS rev01.pdf |

## References to standards

If this document includes references to standards or standardized/ standardizing technical documents the CA allows/permits also another equal solution to be offered.

# Functional, Performance and Design requirements

Functional, performance and design requirements for the mirror substrate are summarized within reference drawing RD-01 (see chapter 1.4).

## General requirements

REQ-033670/A

The Supplier shall produce 1 pc of the mirror substrate with a hole for ELBA beamline in accordance with the requirements given in the reference drawing RD-01 (see chapter 1.4).

REQ-033671/A

The parameters of the mirror substrate shall correspond to the requirements given in the reference drawing RD-01 (see chapter 1.4).

Specific Quality Report: I, II, III, IV (see REQ-033678/A)

REQ-033672/A

The material used for the mirror substrate shall correspond to the requirement from the reference drawing RD-01 (see chapter 1.4) so that no bubbles are present close to the S1 surface. Any other material shall be approved in advance by the CA.

Specific Quality Report: V (see REQ-033678/A)

REQ-033673/A

2 pcs 2” diameter witness samples for damage testing and metrology purpose of the coating run shall be provided by the Supplier.

NOTE 1: There is no specification for the surface flatness. However, the quality of the polish should be 20/10 scratch/dig - exactly the same polishing procedure as the main mirror substrates.

NOTE 2: The witness shall use the same material as the main pieces. Specifications of the leak mirror coating, S- and P-polarization.

## Marking

REQ-033674/A

The mirror substrate shall be marked with bead blasting or by laser engraving according to the reference drawing RD-01 (see chapter 1.4) with character size at least 8 mm.

# Packaging and transport requirements

## General requirements

REQ-033675/A

The mirror substrate shall be cleaned and packaged in the clean environment of class 6 according to ČSN EN ISO 14644 (equivalent to EN ISO 14644) or cleaner.

REQ-033676/A

The mirror substrate shall be placed in a separate PET-G container preventing damage, degradation and contamination. The PET-G containers shall be packed in a minimum of two plies separate clean packaging and placed in a sufficiently padded box for transport.

## Transport

REQ-033677/A

The transportation to the final destination shall be conducted by the Supplier.

# Quality control

## Quality Reports (QRs)

REQ-033678/A

The Supplier shall perform the following tests of product quality and provide corresponding specific quality reports (I - V):

- An interferometric report of the full clear aperture. Sub-aperture measurement is acceptable for spatial periods below 6 mm. At least 2 measurement locations are required for the sub-aperture measurement;

- S-D report listing the main defects and their locations;

- Micro roughness report from the centre of clear aperture. Witness sample processed in the same way can be used too;

- Dimensional report listing the main dimensions;

- Material report showing the Fused Silica class, batch number and producer.

## Documentation and data control

REQ-033679/A

The Supplier shall provide a report about the fulfillment of the technical requirements defined by the product RSD, and completeness of the product (see REQ-033683/A).

REQ-033680/A

The Supplier shall provide the interferometric data from the quality report I (see REQ-033678/A) in a digital form readable by Zygo MX software. Data format shall be agreed with the CA.

## Nonconformity Control System

REQ-033681/A

The Supplier shall establish and maintain a nonconformity control system compatible with ČSN EN ISO 9001 (equivalent to EN ISO 9001).

## Phasing of the delivery

This chapter is intended to briefly summarize basic milestones of the Contract delivery. These milestones represent gates (checkpoints) where the quality of the delivery has to be evaluated.

Delivery shall not proceed past these gates unless their satisfactory accomplishment is approved by the CA.

Delivery lifecycle shall contain at least the following phases (quality gates):

- Manufacturing;

- Acceptance.

### Manufacturing

The goal is to demonstrate that the manufactured product meet the specified technical requirements (RSD) of the CA.

This quality gate concerns primarily:

- Testing at the Supplier’s site (factory testing);

- Packaging.

The output of this phase is a Verified Final Product.

REQ-033682/A

The results of the Manufacturing phase of verification shall be recorded by the Supplier in corresponding QRs (see REQ-033678/A) and provided to the CA for approval (see chapter 4.4.2).

### Acceptance

The Acceptance phase shall demonstrate the following:

- Final product has been successfully verified and this process has been documented in an appropriate way through QRs (see REQ-033678/A);

- All detected nonconformities have been solved in accordance with 
REQ-033681/A;

- Final products are free of fabrication errors.

The output of this phase is an Accepted Final Product.

In case of successful acceptance phase, the CA shall provide to the Supplier signed acceptance protocol. In case of unsuccessful acceptance stage, the CA shall provide to the Supplier Nonconformity Report (NCR) and process in accordance with REQ-033681/A shall be applied.

REQ-033683/A

The verification process shall be carried out by the Supplier and it is successfully completed when the final product comply with all specifications (see REQ-033679/A) and the results of this process are documented in an appropriate way through QRs (see REQ-033678/A).

NOTE: Acceptance will be carried out by the CA on the final products after their delivery to the ELI Beamlines research centre.